## Slide 1
Proprietary and Confidential
1
Title 项目:
Business Challenge 挑战
Problem 面对的问题陈述- 当前BR-IM31 Durm零件取消喷砂后，E-Coating后零件脱皮
Current State 现状
How is this challenge currently tackled, using what technology and are there constraints? 目前如何应对这一挑战、使用什么技术以及存在哪些限制？
热处理后表面产生的物质通过喷砂去除，E-Coating后无脱皮。
Business Drivers 驱动因素 (Key Factors 关键因素)
What do we believe has influence on the phenomenon we are analysing? 我们认为什么会对我们正在分析的现象产生影响？
1.材料 2.热处理前清洗 3.热处理渗碳淬火 4热处理后清洗 5.热处理回火 6.E-Coating所有工序
Objective 目标 (KPIs)
What are we trying to achieve and how will it be measured? 我们想要实现什么以及如何衡量？
取消喷砂后BR-IM31 Durm零件E-Coating后无脱皮
Path to Impact 如何影响:
How will we use the insights / model to achieve impact? How will this be delivered and / or put into production? 我们将如何使用洞察/模型来实现影响？如何将其交付和/或投入生产？
Insights 洞察 –找到减少表面物质和更好处理物质的关键因素，并调整材料、热处理参数、E-coating参数；
Models 模型 – 减少或更好处理钢铁零件表面物质的模型
BUSINESS 业务

## Slide 2
Proprietary and Confidential
2
Target 针对事项
The feature of a dataset that you aim to predict or understand more clearly. (E.g. Quality, Event etc.)
您想要预测或更清楚地了解的数据集的特征。（例如质量、事件等）
-E-coating后零件脱皮
How Target relates to KPI? 针对事项于KPI的关系
-不喷砂的零件E-coating后零件无脱皮就完成KPI
Available Target History 有关针对事项的历史纪录
-有2批的工艺记录
Population 数据填充/量
E.g. Approximately 100,000 process parameter data
-
TRANSLATION 翻译
Title 项目:
Core Data 主数据
Data required to formulate the target 制定目标所需的数据
1.热处理生产工艺记录
2.E-Coating生产工艺记录
Internal Data 相关数据
Data required to corelate & build context 关联和构建上下文所需的数据
1.硬度检测记录
2.E-Coating后零件检测记录
External Data 外部因素的数据
E.g. Material Supplier, Material Grade, Humidity/ Temperature of Environment
-环境的温度和湿度
DATA 数据